## Slide 1
Syndego EnigMAT 65 is an inorganic salt hydrate phase change material-based product with a peak phase changing temperature of 65f. It is incombustible, non-toxic, non-pollutant, long lasting, hydrophobic material with high latent energy. Designed to be specially encapsulated with our patented coextruded polymer film technology but it has outstanding performance for various other applications.
EnigMAT 65
Property | Typical value | Units
Melt/Freeze Temperature | 65/18 | ºF/ºC
Latent energy | 190 | j/g
Specific heat Solid State | 2125 | j/kg/ºK
Specific heat Liquid State | 2080 | j/kg/ºK
Heat Flux Reflectivity – Infrared and Near Infrared wave lengths | 97 | %
Heat Flux Reflectivity – Visible Wave lengths | 86 | %
Emissivity - E | 0.03 | Index (0-1)
Flame spread Index | 5 (25 max) | IN
Smoke developed Index | 10( 450 max) | ppm
Active PCMs | % by weight | 90
Density | 12.85 | #/gal
Melting temperature range | +/- 5 | ºF / ºC
Freezing temperature range | + / - 1 | ºF / ºC
Cycling daily life expectancy | >30 | Years
Reaction to H2O | Hydrophobic | -
The information in this publication is believed to be accurate and is given in good faith, but no representation or warranty as to its completeness or accuracy is made. Suggestions for uses or applications are only opinions. Users are responsible for determining the suitability of these products for their own particular purpose. No representation or warranty, expressed or implied, is made with respect to information or products including, without limitation, warranties of merchantability, fitness for a particular purpose, non-infringement of any third-party patent or other intellectual property rights including, without limit, copyright, trademark and designs.
Syndego LLC reserves the right to make changes at any time without notice.

## Slide 2
Type | 16 oz | 16 oz
Thickness | in | .4
Width | in | 19.5
Length | in | 48
Area weight | # per ft² | 1
PCM Loading | By Weight | 90%
Melt/Freeze Point | Fº/Cº | 65ºF 18ºC
Latent Capacity | Kj/kg | 190
Physical Presentation
Thermal Properties
EnigMAT 65
CALIPER | 4.4 MIL | ASTM D21203
YIELD | 65050 IN2/LB | CALCULATED
PUNCTURE RESISTANCE | 20LBS | MILSTD 3010
TENSILE STRENGTH | 28LBS/IN | ASTM D882
BREAKING STRENGTH | 75LBS/IN (GRAB) | MILSTD 3010
WATER VAPOR TRANS | 0.0005 G/100IN2 DAY | ASTM F 1249
SEAL STRENGTH | 18LBS/IN | ASTM F88
SEALING | Manufacturers Spec | 360º F @ 40PSI 1.5 SEC
Package Properties

## Slide 3
EnigMAT 65
Type | 16 oz | 16 oz
Pallet | inch | 42x48
Product /Pallet | SQFT | 2000’
Net Weight | # | 2000#
20’ container | SQFT | 20,000
40’ container | SQFT | 40,000
Delivery
Waste Management and Disposal
Follow local and national directives for waste management and disposal or regard the following recommendations as a guide:
Deposit packaging materials in appropriate container on site for recycling or reuse.
Avoid using landfill waste disposal procedures when recycling facilities are available.
Keep discarded packaging away from children
Non-warranty
The information in this publication is believed to be accurate and is given in good faith, but no representation or warranty as to its completeness or accuracy is made. Suggestions for uses or applications are only opinions. Users are responsible for determining the suitability of these products for their own particular purpose. No representation or warranty, expressed or implied, is made with respect to information or products including, without limitation, warranties of merchantability, fitness for a particular purpose, non-infringement of any third-party patent or other intellectual property rights including, without limit, copyright, trademark and designs.
Syndego LLC reserves the right to make changes at any time without notice.
EnigMAT 65 is composite solution for general applications which require a high level of insulation and heat storage performance. Each specific application of EnigMAT 65 should require technical analysis of the situation and how the solution will impact the overall desired performance. EnigMAT 65 is designed to interfere with incoming heat fluxes and to downgrade the remaining temperature differential. The leveling of the downgraded temperature is obtained by absorbing and releasing heat above or below its graded temperature.